## Slide 1: PowerPoint 4: The journey of timber
PowerPoint presentation
Unit 108: Wood occupations

## Slide 2: Where does timber come from?
Processes to create joinery and carpentry products
  Woodland or forest
  Harvesting/storage
  Conversion/storage
  Drying the timber/storage
  Rough sawing and grading the timber/storage
  Machining the timber (PSE, CLS)/storage
  Dimensioning the timber/storage
  Manufacturing the product/delivery to site
  Treating, coating timber
  .
Use this style for sources.

## Slide 3: The wood or forest
  Conditions of soil/light
  Coppicing and thinning to maintain healthy trees and underwood
  Effects of wind (minimised in dense forests)
  Rot, infection and burrs
  Parasites and insect attack
  Growth cycles, fast/slow growth

## Slide 4: Conversion methods
Tangential cuts: These are made at a tangent to the grain often through the whole log as in through and through. Also known as crown cuts, the boards are highly figured but are prone to cupping, warping and end splitting.
Radial cuts: The log is sawn at a radial angle into four quarters, hence the name quarter sawn. After that, each quarter is then plain sawn. Has distinctive medullary rays and is more stable than tangential cuts.
Types of cut in log conversion:

## Slide 5: Types of log conversion
Through and through (crown cutting): Produces wide tangentially cut boards. The easiest milling process as you don’t need to turn the log.
Quarter sawn: Traditional method to produce radial boards. Time consuming but a much more stable product.
Through and through
Quarter sawn

## Slide 6: Types of log conversion
Boxed heart: Boxed heart is a combination of other methods but avoiding the heart of the tree. This method is used if the heart of the tree is defective (i.e. rotted).
Tangential: Used for structural timbers (like floor joists) as the grain configuration makes the most of the tree ring’s strength. In the image shown here, the heart is boxed.
Boxed heart
Tangential

## Slide 7: Stacking and seasoning
Before most timber is usable, it must lose 50% of its felled water content to avoid getting rot, become stronger and lighter, avoid shrinkage after fitting and allow it to be coated. Dried timber must have a maximum water content of 20% or less to avoid getting wet rot. Seasoning is done in two ways:
Air drying: Timber is stacked flat and separated by ‘stickers’ for even air circulation. It is then covered to protect from rain and UV and allowed to air dry normally for a year per inch of thickness. Air drying is limited to reducing overall moisture to 14% (not enough for some internal joinery).
Kiln drying: Timber is stacked and separated by ‘stickers’ for even air circulation then dried slowly in a heated kiln for 10 hours to 28 days depending on type and thickness. This reduces overall moisture to 20% or even down to 6% (required for internal joinery near sources of heat).
cornwallhardwoodsupplies.co.uk

## Slide 8: Grades of timber
Scant: (Scandinavian timber) slow grown spruce (whitewood) C16
CLS: (Canadian lumber standard) semi finished, eased edge timber C16
C16/24: strength ratings based on the rate at which the timber grows and can withstand stresses. (more growth rings=stronger timber)
PSE: (planed, square edged) normally applies to redwood that has been planed square for interior use from rough sawn
Rough sawn carcassing timber: commonly sized in inches, unfinished
Waney edged timber: large rough sawn planks, often with the bark still attached after being through and through sawn
cornwallhardwoodsupplies.co.uk

## Slide 9: Stress testing and grading
The British Standard BS 5268 states there are 12 strength grades, but the most widely used are C16 and C24. Both grades are used in structural applications and are suited to different loads. They are used for floor joists, rafters, structural studwork, partition walls, and formwork and shuttering.
Methods of grading: before timber is sold as a building product it is often stress tested to grade it for strength. It is then machined to certain standard dimensions to suit its application, such as CLS and Scant which are known as ‘regularized’ timber.
C16 stamp
C24 stamp

## Slide 10: Timber defects
Shakes: caused through rapid drying creating splits in timber normally at the end of a plank, sometimes called checks.
Split: when a shake travels the length of the plank splitting it.
Upset (thunder shake): a crack or weakening across the width of a plank caused by a sudden shock compressing the fibres, as with thunder or lightning, severely reducing the strength.
Star shake: a star shake is caused by rapid or uneven seasoning, causing the outside of the log to shrink faster than the heart. Exposure to the elements can cause star shakes, as can frost during the growth of the tree.
Thunder shake
Star shake

## Slide 11: Timber defects
Cup shake a cup or ring shake follows the growth rings and can be caused by the growth of the tree or bending or twisting in winds.
Heart shake: a heart shake is a crack near the heart of the tree caused by poor seasoning, or by using trees felled past maturity.
Frost shake: caused by moisture getting into the timber and expanding and forcing the grain apart.
Collapse: caused by rapid drying causing the timber to lose strength.
Case hardening: caused by rapid drying, causing the outside to harden while the inside remains damp,
Knots: naturally created weak points or voids caused by branches and twigs growing from the tree.
Dry rot: can attack any timber if it has a single water source like a leak and can travel through stone, killing all timber and reducing it to a white powder. It can travel through airborne spores or vine-like tendrils.

## Slide 12: More timber defects
Wet rot: wet rot can attack timber with 20% moisture content or more. The timber affected is attacked by fungus and decays into a mushy dust.
Blue stain: naturally occurring fungus when moisture content is above 20% causing discoloration.
Resin pocket: a hollow pocket filled with resin as found in the majority of softwoods.
Spiral grain: resulting from stresses on the tree while growing, including its position and environmental conditions
Honeycombing: honeycombing occurs in the inner part of the wood, which cannot always be identified by eye. It can be due to stresses developed during the drying of timber.
Wet rot
Honeycombing

## Slide 13: Timber deformities
Bowing: normally caused by uneven tension as a result of poor drying and stacking or can be cut from bent stock.
Crooking: normally caused by uneven tension as a result of poor drying and stacking, or was ripped from a bowed piece of stock using pressure.
Cupping: normally found in tangential cuts caused by uneven tension on opposing faces.
Twisting: normally caused by twisted grain as the tree grows, sometimes caused by strong winds or can be caused by uneven drying and poor stacking.
Waney edge: when the bark and sapwood are visible along the edge of the timber.
Bowing
Cupping
Twisting

## Slide 14: Types of finish
Bare wood
Primer
Gloss paint
Satin paint
Varnish
Oil
Wax

## Slide 15: What are the benefits of using timber over other materials?
    Timber is a regenerative source of building materials and is therefore eco friendly.
    Timber can be repaired easily, often with no visible evidence of damage.
    Timber can be treated and finished to protect it with natural products, such as oils and waxes.
    Timber looks beautiful and has a living, warm appearance compared to other materials.
    Timber has good insulative properties and can last a long time if looked after.
    Timber is highly workable and takes well to adhesives and fixings.

## Slide 16
Any questions?