## Slide 1: PowerPoint 14: Concrete place and compact
PowerPoint presentation
Unit 112: Construction operations and civil engineering operations

## Slide 2: Pre-pour!
Before concrete placing begins, the insides of the forms should be inspected to make sure they are clean and have been treated with release agent. If the forms are deep, temporary openings and lighting may have to be provided for this inspection.
Rubbish, such as sawdust, shavings and reinforcement tying wire, should be blown out with compressed air. Any rainwater at the bottom of the form should be removed. Similarly, the reinforcement should be inspected to check that it complies with the drawings and that the correct and sufficient numbers of spacers have been used.

## Slide 3: Concreting in cold weather
Water expands when freezing. This can cause permanent damage if the concrete is allowed to freeze when freshly laid or in hardened concrete that has not reached enough strength. Concreting should not take place when the temperature is 2˚C or less.
If the temperature is only slightly above 2˚C, the mixing water should be heated.
After being laid, keep the concrete warm by covering it with insulating quilts. This allows the cement to continue its reaction with the water and prevents it from freezing.

## Slide 4: Placing the concrete
There are different methods for transporting concrete on site, ranging from hand wheelbarrows to concrete pumps.
The choice of method will depend on the size and complexity of the project, and factors such as ground conditions and distance to be covered and the availability of cranes or other plant. On many jobs several different methods, or even a combination of methods, may be required.
Concrete must be moved to the point of placing as quickly and economically as possible without allowing setting, segregation, loss of consistence, loss of any ingredients, contamination with water, or any other material, after it has left the delivery tank.

## Slide 5: Placing methods – pumping
Pumps were first used to transport and place concrete in in the 1930s, and a significant amount of concrete is now placed in this way. Many pumps are capable of moving up to 200m³ per hour, depending on the pump type, the horizontal and vertical length of the pipeline, the number of bends and the consistence of the concrete.
In practice, the output of a modest-sized pump is usually about 50m³ per hour due to supply and organisational limitations. By comparison, a crane with a 1m² skip and a 5-minute turnaround cycle can deliver only 12m³ per hour.
www.youtube.com/watch?v=Puxt1c7GoDs
www.youtube.com/watch?v=t5e0anH2IUk
YouTube Link

## Slide 6: Placing methods – crane and skip
The crane is still probably the most common method of handling concrete for combined vertical and horizontal movement. A crane is frequently needed on site for handling formwork and reinforcement, and its further use in transporting concrete may be both economic and convenient. However it may be more cost-effective to transport the concrete by other means.
Skips generally range in capacity from 0.2 to 1.0m³ and are broadly of two types.
Lay-back or roll-over skips.
Constant attitude skips.
www.youtube.com/watch?v=f17dQUOZY64 http://www.youtube.com/watch?v=11qRE5fWFVk
YouTube Link

## Slide 7: Placing methods – dumper
Dumpers, generally of approximately 0.5m³ capacity, are a common form of transport on many construction sites where direct access to the works is not possible. They may be discharged either forward or sideways and are best when hydraulically operated so that the discharge can be controlled.
The main disadvantage of gravity discharge is the sudden uncontrolled surge of concrete – the heavy impact can displace reinforcement and other objects in the formwork. For small sections, it may be necessary to discharge onto a banker board first and then shovel in the concrete by hand.
www.youtube.com/watch?NR=1&v=XSYVTN-bVBs&feature=endscreen
www.youtube.com/watch?v=qeA3zm7aJik
YouTube Link

## Slide 8: Placing methods – others
There are other ways of placing or pouring concrete to its required location:
Straight from the concrete wagon chute
www.youtube.com/watch?v=qOVgphzeHsY www.youtube.com/watch?v=DLIWAbA0fc0.
Conveyor belt
www.youtube.com/watch?v=dpA5zfzViYw www.youtube.com/watch?v=GRojfcaqna4
Wheelbarrow
www.youtube.com/watch?v=RRuUd_ps1zo www.youtube.com/watch?v=DrevoR2fRjA
YouTube Link

## Slide 9: Compaction
After concrete has been mixed, transported and placed, it contains entrapped air in the form of large voids. The object of compaction is to get rid of as much of this air as possible. Before compaction, concrete may contain more than 5% entrapped air and in some mixes it may contain as much as 20%.

## Slide 10: Compaction
If this entrapped air is not removed by proper compaction the presence of these large voids will:
reduce the strength of the concrete: more than 5% loss of strength for every 1% air
increase the permeability and hence reduce the durability and protection to the reinforcement
reduce the bond between concrete and reinforcement
result in visual blemishes, such as excessive blowholes and honeycombing on formed surfaces.
Fully compacted concrete will be dense, strong, impermeable and durable.

## Slide 11: Compaction
To compact such concrete satisfactorily, a mechanical method of vibration must be used, applied internally in the concrete, externally on the forms or on the surface of the concrete.
The vibrating plant selected will be determined by the type of work under construction, the density of the reinforcement and the workability of the mix.
Vibrators are available driven by petrol, diesel, electricity or compressed air.

## Slide 12: Compaction
Most concrete is compacted by means of the immersion type vibrating poker.
All pokers, except air operated and some electrical models, have a long flexible drive shaft which is driven by a portable power unit.

## Slide 13: Compaction – pokers
When the poker is inserted in the concrete, the area of effective vibration is within the area that air bubbles are seen to blow on the surface, and laitance forms. This is termed the radius of action.
When compaction is taking place a system of overlapping vertical insertions of the poker must be made and at each position withdrawn slowly to allow the holes formed to close up.
The length of time a poker should be left in the concrete before moving to the next position is a matter of experienced observation. When the air bubbles cease to appear on the surface and the poker sound frequency drops to a constant pitch, the concrete is free of entrapped air.

## Slide 14: Compaction – pokers
Each layer should be placed and compacted without delay to obtain a complete homogeneous concrete and in most instances the use of more than one poker vibrator will be necessary.
The concrete should be placed and compacted in equal layers not exceeding the depth of the poker and when each layer is compacted the poker should just penetrate into the lower layer.
www.youtube.com/watch?v=CYS99cPi96E
YouTube Link

## Slide 15: Compaction – beam vibrators
Consist of a single timber or twin metal beam onto which a vibratory motor/motors is mounted.
Used to compact road or floor slabs, the beam spans across from the edge forms to consolidate and screed the concrete level as it passes over the surface.
Some models available can be tensioned to form a camber if required. Can compact workable concrete satisfactorily to at least 150mm thickness but the equipment is generally used in conjunction with the poker vibrator.

## Slide 16: Compaction – beam vibrators
When using hand-held vibrating beams, little or no compactions will take place near the edges or around formed joints. It is necessary to use an internally vibrating poker in these areas to ensure complete compaction of the whole slab.
www.youtube.com/watch?v=Hc48x7ZgVM8
www.youtube.com/watch?v=ONwzdP4kUw8
www.youtube.com/watch?v=lgPS_yOuDjE
YouTube Link

## Slide 17
Any questions?