## Slide 1: PowerPoint 16: Concrete finishing
PowerPoint presentation
Unit 112: Construction operations and civil engineering operations

## Slide 2: Standard of finish
Concrete can be produced within close dimensional tolerances, but with different variations in colour and the presence of marks and ridges, depending on the method of finishing, the surface will rarely be entirely blemish-free. It is unrealistic to expect perfection in appearance.
For some finishes it may be essential to cast a bay as a sample in order to avoid later dispute about the quality of the work. To judge the quality of the finish, the sample should be viewed at the same distance from which the job will be seen, bearing in mind the actual in-service conditions and the floor covering where applicable.

## Slide 3: Choice of finish
The finish of a concrete floor should be chosen after considering the type of traffic, loading, impact abrasion and chemical resistance that is likely to be applied to the floor. If subsequent surface finishes are to be applied, such factors as hygiene, dust prevention, slipperiness and decorative treatment should also be considered.
To achieve good regularity of the final surface it is essential to provide accurately set and levelled square-edged side forms, and to give careful attention to concrete placing, compaction and levelling.

## Slide 4: Finishes – float (smooth)
This is normally the first finishing process after the surface has been compacted and levelled. Floating closes up the surface of the concrete by spreading the mortar over the top of the coarse aggregate. A skip-float consists of a large narrow float on the end of a long handle. This is skimmed over the surface of the fresh concrete, probably two passes only. The float is able to tilt by means of rotating the handle so that it easily glides over the concrete surface in both directions. The result is a surface that has ridges and float marks which may not be suitable for the direct application of thin flooring materials.

## Slide 5: Finishes – tamped
A texture can be applied by imprinting the fresh concrete using a tamping beam. In its simplest form, the beam is moved across the levelled surface in a series of close up and down horizontal movements. The frequency and amplitude of the ridges produced will depend on the thickness of the beam, the concrete consistence and the skill of the operatives.

## Slide 6: Finishes – brushed
This finish is achieved by pulling a brush over the surface of the wet concrete after the surface has been levelled. The finish obtained will depend on the harshness of the bristles or tines on the brush and the consistence of the concrete.

## Slide 7: Finishing – power float
After the surface has been levelled, the surface is power-floated to smooth and close the previously levelled concrete surface after it has stiffened sufficiently – about three hours after laying. This process, often called 'panning’, involves the use of a power float which has a rotating circular disc attachment or large flat individual blades. The finish is not highly polished and gives characteristic swirl marks with a sandpaper/gritty texture to the surface.

## Slide 8: Finishing – power trowel
A power-trowelled finish is obtained by first using a power float. After a delay to allow excess surface moisture to evaporate, the slab surface is further smoothed and made dense with a power trowel to provide a smooth, polished appearance. A power trowel has tilted individual blades that are smaller than the power float and is used for final finishing. For industrial floors, dry-shake hardeners are used to give greater abrasion resistance and pigmentation. The material is spread onto the fresh concrete and power-floated and trowelled to form a monolithic topping. The timing of each operation is critical.

## Slide 9: Finishing – power-grinding
Power-grinding is a finishing technique intended to provide an acceptable and durable concrete wearing surface without further treatment. After the concrete has been fully compacted and accurately levelled with a double-beam vibrator or similar, it is further smoothed with a skip-float.
The concrete is allowed to harden and the surface is then ground to a coarse 'sandpaper‘ texture using a low-speed grinder to remove the top 1–2mm of laitance and mortar as well as minor irregularities left during finishing. The grinding is not intended to remove gross inaccuracies of level. The age of the concrete at grinding depends on the gain of concrete strength, but for maximum economy grinding is usually carried out between one and seven days after laying, as soon as the concrete can be ground without tearing fine aggregate particles from the surface.

## Slide 10: Finishing – polished
Concrete can be polished by grinding to varying degrees of smoothness, from matt to high gloss. The latter can have the appearance of marble or polished granite. The polishing of small components is generally carried out with hand-held tools, but larger units are polished mechanically. Grinding away the outer 2 or 3mm will reveal the aggregate. The final finish depends on the fineness of the abrasive polishing heads and the number of times that they are passed over the concrete surface.
The final process involved in internal polished concrete is the application of a surface sealer to give a durable, longwearing protective coating. Sealants can take the form of wax, solvent or water (acrylic) based products, all of which can be clear or coloured.

## Slide 11: Finishes
There are various other finishes. Here are just a few more examples:
Exposed aggregate

## Slide 12: Finishes
Sand blasted

## Slide 13: Finishes
Other finishes include:
Patterned Imprinted

## Slide 14: Finishing tools and stencils
Stencilled
Crimper or brass indent roller

## Slide 15: Some examples of how it is done
Installing a concrete drive (brush finish) concrete drive
www.youtube.com/watch?v=xUgiHghs8vs
Using a power trowel
www.youtube.com/watch?v=LkTre1zo85w
Ride-on power trowel
www.youtube.com/watch?v=0eXXRhp0p3w
YouTube Link

## Slide 16
Any questions?