## Slide 1: PowerPoint 10: Preparing backgrounds
PowerPoint presentation
Unit 116: Wall and floor tiling

## Slide 2: Aim: To give learners an understanding of preparing backgrounds used for wall and floor tiling. Outcomes: At the end of this session, the learner will be able to: Outcome 1: Identify a range of methods for preparing different backgrounds. Outcome 2: Have an awareness of the importance of compatibility between backgrounds and applied materials. Outcome 3: Identify surface characteristics, such as dryness, flatness, rigidity, true and square, plumb, level and soundness.
PowerPoint presentation

## Slide 3: Preparing backgrounds
In construction, there are many different types of backgrounds that a wall and floor tiler will encounter, while fixing wall and floor tiles.
What is a background?
A background is any wall or floor construction that a tiler fixes wall and floor tiles to.

## Slide 4: Preparing backgrounds
Caution!
Part of a wall and floor tiler’s work is involved with preparing background surfaces in existing buildings.
Older buildings contain materials that are no longer in use but which are toxic and/or hazardous to health.
Removing old existing background surfaces can cause dust, which when breathed in, may cause health problems, sometimes many years later.

## Slide 5: Preparing backgrounds
Some of the hazards that are common in older buildings are:
Asbestos: found in thermoplastic floor tiles, artex, pipe lagging and toilet cisterns and many other components and materials.
Lead: found in paint.
Arsenic: found in old green wallpapers.
VOC (Volatile organic compounds): found in plastics and protective coatings.
Fibreglass: may be present when replacing upstairs ceilings.
Silica: found in stone, sand, tiles and bricks, and can be inhaled from cutting masonry.

## Slide 6: Surface characteristics
Surface characteristics can be defined as:
dryness
flatness
rigidity
true and square
plumb and level
soundness.

## Slide 7: Surface characteristics: dryness
In preparation for tiling, a background must be dry.
New plaster walls (gypsum-based)
New render walls (cement-based)
New screeded floors (cement/gypsum-based)
New concrete floors (cement-based)
Newly finished backgrounds need to be fully cured before any tiling preparation work.
BS 5385-1:2018 Sufficient additional time should be allowed for curing, commensurate with the extent of making good, before using the chosen bedding system.

## Slide 8: Surface characteristics: rigidity
All materials have a level of measurable strength, linear, compressive, tensile and shear.
An example of rigidity is the thickness of a plasterboard being 12.5mm compared to 9.5mm. The 12.5mm thick plasterboard will be the more rigid of the two sizes.

## Slide 9: Surface characteristics: true and square
In construction, for something to be true, means it is exact or accurate.
Square, in measurement, is a device consisting of two straight edges set at right angles to each other. A tiler will use a square to set out floor tiling or to mark tiles ready for cutting.
Steel
square
Setting out using the 3:4:5 method

## Slide 10: Surface characteristics: plumb and level
Definition of plumb: a lead weight attached to a line and used to indicate a vertical direction so out of plumb or off plumb means out of vertical or true. /
Tilers use plumb and level when setting out tiling to establish level datum lines and vertical centre lines, by means of using a spirit level, laser level or a plumb bob.

## Slide 11: Surface characteristics: plumb and level

## Slide 12: Surface characteristics: soundness
Plasterboard, cement board and timber floor boarding must be secured with the correct fixing methods and fixings, such as screws/nails.
A solid/strong background will ensure the tile work to be fixed will not come loose, crack or fail.

## Slide 13: Types of backgrounds: new and existing areas
Gypsum based Timber (flooring) Cement based

## Slide 14: Types of backgrounds: new and existing areas
      Wall and floor tiling is carried out in many different environments, including domestic, commercial and industrial types of construction (building) sites.
      These construction (building) sites provide wall and floor tiling for new housing, shops, restaurants, offices, hospitals and many other building types.
      Wall and floor tiling is also needed within existing buildings where refurbishment and renovation works are required.
      New and existing buildings have a variety of different building material backgrounds relating to their design.

## Slide 15: Gypsum-based backgrounds
    Gypsum-based backgrounds on walls are plasterboard and plaster. Plaster can be applied to plasterboard and to sand and cement render.
    According to BAL (British Adhesives Limited), the maximum weight of tiles that can be fixed to gypsum-based backgrounds are:
    Tiling on plasterboard without a plaster skim means an extra 12kg of weight can be fixed to it.
https://www.tiles.org.uk
Note: 12.5mm Plasterboard (rigidity)
Wall substrate | Maximum weight of tiling per m2
Gypsum plaster | 20kg
Gypsum plasterboard Skimmed (12.5mm thickness) Unskimmed (12.5mm thickness) | 20kg 32kg

## Slide 16: Gypsum-based backgrounds
    Plasterboard can be tiled directly on to, which may need one undiluted coat of primer, but a plaster skim coat will need to be primed twice with an undiluted acrylic based primer. Source: BAL site guidance information.
Before tiling, certain wall and floor (Anhydrite screed) backgrounds/substrates may require priming to reduce the porosity and suction. Priming will improve the bond between the substrate and the tile being fixed by an adhesive.
Some cement-based adhesives have been specially formulated for use on suitably primed gypsum plaster. As with all plaster backgrounds, success is very dependent on the plaster being sufficiently strong and dry throughout.
BS 5385‑1:2018

## Slide 17: Gypsum-based backgrounds
    Gypsum-based (calcium sulphate, see note below) backgrounds on floors are known as Anhydrite screeds which are a form of flow/liquid screed types.
    From the chemical point of view anhydrite is anhydrous calcium sulphate (CaSO4) – a binder which is very similar to gypsum (formed by dihydrate calcium sulphate – 2H2OCaSO4). https://www.atlas.com.pl
While similar to a gypsum-based background, special care is needed to prepare this type of background prior to floor tile installation.
https://liquidscreedflow.co.uk

## Slide 18: Gypsum-based backgrounds
See information at
https://www.tiles.org.uk/tiling-guide/
for tiling on anhydrite screeds

## Slide 19: Cement-based backgrounds
    Cement-based backgrounds (cement-based backer boards), concrete, screed and render are composed of materials such as:
    cement
    sand (fine aggregate)
    chippings (coarse aggregate)
    These materials are mixed in various ratios according to the purpose they are designed for:
    concrete ratio 1:3:6
    screed ration 1:4
    render ratio 1:4

## Slide 20: Cement-based backgrounds
    Cement-based backgrounds provide a strong and durable surface that can be fixed over wood floors and on to walls. They can be rot, swelling, warping and moisture resistant, and provide excellent protection in wet areas. They can be fixed to the background substrate using the appropriate fixings and/or thin bedding them to floors.
    Cement-based backgrounds that wall and floor tilers work with include:
    cement-based backer boards, solid and insulated (foam core)
    sand and cement, semi-dry screed
    concrete
    render.

## Slide 21: Cement-based backer boards, solid and insulated (foam core)
    Cement-based backer boards are manufactured as solid, and as a foam core sandwiched between two layers of reinforced cement-based material.
    There are pros and cons to each system and different methods to prepare and fix the boards to the building substrate, such as to floors and stud partitions.

## Slide 22: Solid cement-based backer boards
    This type of board, as the name suggests, has been manufactured as a solid material product. It is advisable to prime the surface prior to tiling.
Pros | Cons
Moisture resistant | Heavy
Warp resistant | Harder to cut than foam core boards
Load bearing | 
Heat resistant | 

## Slide 23: Insulated (foam core) cement-based backer boards
    This type of board, as the name suggests, has been manufactured from an extruded polystyrene foam core and finished on both sides with a cement-based material. It is advisable to prime the surface prior to tiling.
Pros | Cons
Moisture resistant | Not used in hot environments
Warp resistant | Holds less weight than solid board
Used with underfloor electric heating | 
Lightweight | 
https://www.jackon-insulation.co.uk

## Slide 24: Cement-based backgrounds: screed
    This type of background is constructed to provide a smooth and flat flooring surface to a datum level (finished floor level, FFL) in preparation to receive a floor finish product.
    Concrete is composed of:
    cement
    sand (sharp type)
    clean water.
Cement screed needs to be primed with an acrylic primer prior to floor tiling.

## Slide 25: Cement-based backgrounds: concrete
    This type of background is constructed to provide a smooth and flat flooring surface to a datum level (finished floor level, FFL) in preparation to receive a floor finish product.
    Concrete is composed of:
    cement
    sand (fine aggregate)
    chippings (coarse aggregate)
    clean water.
A concrete floor slab should be checked for level/flatness and primed with an acrylic primer prior to tiling.

## Slide 26: Cement-based backgrounds: render
    Render is a type of background, consisting of around a 1:4 cement and sand mix ratio, applied by a plasterer to walls, consisting of two coats.
    Render can be applied internally and externally. It can be finished in a variety of ways. For tiling, a fine down finish is required.
    As a tiling background, render needs to be dry, flat, sound and have a light key referred to as a devil float (1mm surface scratch), as well as being primed with acrylic primer prior to fixing wall tiles.

## Slide 27: Cement-based backgrounds: render
Sand and cement render
being applied to a brick wall
https://www.bunnings.com.au/

## Slide 28: Timber-based backgrounds
    Timber is used in a wide range of applications in the construction of buildings, from flooring, doors, skirting, architraves, joists and roof structures.
A tiler will often have to tile a floor which has been constructed out of timber, but must be aware that according to BS 5385‑1:2018, 6.2.3, ‘Sheets and boards subject to movement from changes in moisture content, such as plywood, chipboard, wood partial boards, etc., should not be used.’
Timber structural floor boards
Moisture resistant chipboard sheeting

## Slide 29: Timber-based backgrounds
Tiling to timber based backgrounds is not good practice and advised against according to British Standards.
When tiling to a timber floor background, an uncoupling or decoupling membrane should be installed over the existing floor surface.
What is an uncoupling membrane?
An uncoupling membrane system provides an intermediate substrate between the tile covering and load bearing substrate. They can be used over a variety of substrates, which include timber, concrete, cementitious screeds and gypsum based screeds. They are designed to neutralise lateral stresses that occur between the substrate and tile covering; they are not designed to accommodate differential vertical movement (deflection).
Source: https://www.schluter.co.uk

## Slide 30: Timber-based backgrounds
How does an uncoupling membrane work?
The membrane works by preventing stresses from the substrate being transferred into the tile covering that can cause cracking and delamination of the covering material.
As substrates will expand and contract due to changes in temperature and moisture levels, an uncoupling membrane is perfect for allowing the surfaces to move independently preventing stress on the tiles which can cause cracking or even debonding. This is because the membrane uncouples the floor covering from the substrate and neutralises the tensions between the substrate and the tile covering that result from the varying deformations of the materials. Likewise, stress cracks in the substrate are bridged and are, therefore, not transferred to the surface covering.
Source: https://www.schluter.co.uk

## Slide 31: Timber-based backgrounds (uncoupling membrane installation)
© 2021 Schlüter-Systems Ltd
Acrylic primer is applied to the timber substrate.
The decoupling membrane is fixed to the timber substrate with flexible adhesive.
It is left to set.
Tiling is fixed to the membrane with flexible adhesive.

## Slide 32
Any questions?