## Slide 1: PowerPoint 8: Characteristics of materials and resources within wall and floor tiling
PowerPoint presentation
Unit 116: Wall and floor tiling

## Slide 2
Aim: To give learners an understanding of the materials and resources used in wall and floor tiling.
Outcomes: At the end of this session, the learner will be able to:
Outcome 1: Identify and describe the characteristics of materials and resources.

## Slide 3: Materials and resources used in wall and floor tiling
Ceramic tiles
Porcelain tiles
Plastic (PVC) trim
Adhesives (ready mixed and powder-based)
Cementitious grout (ready mixed and powder-based)
Primers
Bonding agents
Levelling/smoothing compounds
Sealants
Decoupling membranes

## Slide 4: Ceramic tiles
Ceramic tiles fall into two categories, according to their method of manufacture.
Extruding tiles: whose body is shaped in the plastic state in an extruder and the resulting column cut into tiles of predetermined thickness.
Dry-pressed tiles: which are formed of powder or small grains, shaped in moulds under high pressure before firing. These tiles are generally are made to finer dimensions than extruded tiles.
Source: Annex A British standards BS 5385

## Slide 5: Ceramic tiles
3
A ceramic tile is made up of clays and other materials. The main body of the tile is called the bisque (or biscuit), and the face side can be glazed, partly glazed, unglazed (better for slip resistance), polished, textured or profiled.
Ceramic tiles are manufactured in a range of sizes and thicknesses and are predominantly of square or rectangular shapes, but other geometrical shapes are available.
Note: Ceramic tiles can be fixed using dispersion-based and cement-based adhesives.

## Slide 6: Ceramic tiles
Ceramic tiles are suitable for fixing to walls and floors, but not all ceramic tiles can be used for floor applications. This is because most types of ceramic tiles have a higher water absorbing property, making them weaker than porcelain tiles.
Glazed ceramic
Un-glazed ceramic

## Slide 7: Porcelain tiles
These are highly attractive and very hardwearing tiles that have extremely low water absorbency. Available as wall or floor tiles, sometimes glazed, often with good anti-slip properties, they can be used internally and, providing they are of sufficient slip resistance, externally. These tiles are, depending on thickness, suitable for domestic and commercial use. They typically require the use of a polymer enhanced cement based adhesive. The use of a ready-mixed adhesive is not recommended.
https://www.tiles.org.uk/

## Slide 8: Porcelain tiles
Porcelain tiles are manufactured using heavy, dense, usually white clays mixed with sand feldspar.
Because of this density, porcelain tiles are an excellent choice for floors and used in high foot traffic, commercial, industrial and wet areas such as wet rooms.
Porcelain tiles

## Slide 9: Plastic (PVC) trim
The purpose of a wall tile profile (trim) is to provide both protection and decoration to exposed tile edges. Source: British standards BS 5385
Trim comes in many sizes, relating to the thickness of the tile being used.

## Slide 10: Plastic (PVC) trim
Trim is used around the perimeter of window and door openings, and external corners to columns and boxing in around pipework.
© 2021 Schlüter-Systems Ltd

## Slide 11: Adhesives (ready mixed and powder based)
Tile adhesive is the material that is used to create a mechanical bond between a background surface, such as a wall or floor, and a wall and floor tile.
Before any tile adhesive is applied, there are some important factors to determine, such as:
the size of the tile to be fixed
the size of the trowel to be used (notch size)
the type of adhesive to be used, and mix ratio
the method of application of the adhesive.

## Slide 12: Adhesives (ready mixed and powder based)
The size of the tile to be fixed directly relates to the size of the trowel to be used (notch size).
Round notched trowel edge profile: 6mm round notches at 12mm centres. Coverage: approx. 70%. Use for: thin-bed fixing, interior dry areas. Tiles: most ceramics/marble/natural stone wall tiles under 300mm in size.
Example 1

## Slide 13: Adhesives (ready mixed and powder based)
The size of the tile to be fixed directly relates to the size of the trowel to be used (notch size).
Mosaic trowel edge profile: 4mm square notches at 8mm centres. Coverage: approx. 90% to 100%. Use for: thin-bed fixing. Tiles: mosaics/wall and floor tiles up to 100x100mm and fixing uncoupling membranes.
Example 2

## Slide 14: Adhesives (ready mixed and powder based)
The size of the tile to be fixed directly relates to the size of the trowel to be used (notch size).
Thick bed solid bed trowel edge profile: 20mm round notches, 10mm deep, at 28mm centres. Coverage: 100% achievable at
3–4mm bed depth. Use for: solid-bed fixing. Tiles: most wall and floor tile types (with recessed/keyed back patterns). Ideal for fixing large format wall tiles and up to 300mm floor tiles.
Example 3

## Slide 15: Adhesives (ready mixed and powder based)
Another important factor when preparing adhesives for tiling installations is to determine the type of adhesive.
There are two main types.
Dispersion-based (ready mixed): this type of adhesive is used with ceramic tiles and not to be used with porcelain tiles.
Powdered-based (cement-based): this type of adhesive should be used with porcelain tiles and can be used with ceramic tiles.

## Slide 16: Adhesives (ready mixed and powder based)
The method of application of the adhesive is important to get right so as to ensure the tile is fixed firmly to the background surface.
Adhesives should be spread evenly with a suitable notched trowel.
Dot and dab is not an acceptable method of fixing tiles on either walls or floors.
Good tile coverage reduces the risk of tiles coming away from the background.

## Slide 17: Adhesives (ready mixed and powder based)
https://www.tiles.org.uk/tiling-guide/
Adhesive should be applied straight and in one direction.
Straight
Allows air to escape and good compression of tile
Swirl
Traps air which can hinder compression
Dot and dab
Creates weak points in the tile

## Slide 18: Cementitious grout (ready mixed and powder based)
Tile grout is the material tiler’s use to fill the joints formed between tile work. Grout joints can range from 2mm to 20mm, and the quantity of linear metres of grout joints can vary dependent upon the tile size.
Before any tile grout is applied, there are some important factors to determine, such as:
the type of grout needed for the work being carried out
the quantity of grout needed
the colour
the method of application of the grout
the width of the grout joint.

## Slide 19: Cementitious grout (ready mixed and powder based)
The type of grout needed for the work being carried out can be:
ready mixed
cement-based: following the instruction on the packaging, grout must be mixed to the specified ratio with cold clean water.

## Slide 20: Cementitious grout (ready mixed and powder based)
The quantity of grout needed: this information can be found on the packaging.
For example, if using a 10kg bag of BAL grout: on the back of the grout bag, under the heading ‘coverage’, you will see:
This 10kg bag of grout covers:
35.500m² with 300x300x9mm tiles with 3mm joints
24.000m² with 200x200x9mm tiles with 3mm joints.

## Slide 21: Cementitious grout (ready mixed and powder based)
The colour: grout is available in many colours to match tile colour and personal preference.
As there are many colours this benefits renovation works where a suitable match may be found.

## Slide 22: Cementitious grout (ready mixed and powder based)
The method of application of the grout is important.
Before grouting starts, ensure that the adhesive
is fully hardened to avoid disturbing the tiles before
they have bonded completely with the adhesive. Check the setting time of the adhesive used.
When mixing a powder grout with water, always use the correct and consistent amount of water to avoid shade variation.

## Slide 23: Cementitious grout (ready mixed and powder based)
Apply the grout into the joints using a squeegee.
Once in the joint, the grout should be left to firm before
cleaning down. This is to ensure it remains in the joint
and does not absorb significant levels of extra moisture
when the area is cleaned.
Cleaning off too early can affect the colour consistency, creating a patchy colour appearance and can also affect the grout strength,
leaving a weak, dusty surface layer.

## Slide 24: Cementitious grout (ready mixed and powder based)
Relation between grout width and tile size
Grout joints are not just a sealed gap between fixed tilework, their widths
are determined by the size of the tile being used.
Stated in the British Standards, BS 5385-1 2018 (7.1.1):
Minimum grout widths vary by tile facial area, examples include the
following.
For tiles with the facial area <0.1 m² with no side over 600 mm long,
joints should be not less than 2mm wide;
Tiles with a facial area 0.1 m² to 1 m² with no side over 1.200mm
long, joints should be not less than 3mm wide.
This informs us that a grout joint acts also as a movement joint.

## Slide 25: Primers
Correct substrate preparation is essential for successful tiling installation. All background surfaces need to be clean, dry and free of contaminates such as dust and any debris.
Priming may be required to improve the bond to some surfaces.
Primers stabilise dusty surfaces and reduce the porosity of the background prior to fixing tiles.
The type of primer to use when tiling is acrylic primer, not PVA.

## Slide 26: Primers
Primers are applied to background surfaces using a brush or roller and tray.

## Slide 27: Primers
It is important to remember when using a primer that the instructions on the packaging/container must be followed to ensure the product is being applied correctly.
Check the type of background.
Check the adhesive is compatible with the primer.
Make sure the correct mix ratio of primer to water is understood.
Follow safety advice when using construction chemicals.

## Slide 28: Bonding agents
Bonding agents are used in cement-based mortars and adhesives to improve the physical performance, including adhesion, durability, flexibility, waterproofing and workability.
The most commonly used type is a water-based dispersion of styrene butadiene copolymer (SBR) or acrylic polymers.

## Slide 29: Bonding agents
Added to the mix, it is recommended to follow the manufacturer’s instructions to achieve the correct mix ratio and safety advice while using building chemicals.

## Slide 30: Levelling/smoothing compounds
Correct substrate preparation is essential for successful tiling installation. Floor surfaces need to be clean, dry and free of contaminates such as dust and any debris.
Priming may be required to improve the bond to some surfaces.
Levelling compound fills small uneven areas on the floor surface, providing a smooth flat finish prior to floor tiling.

## Slide 31: Levelling/smoothing compounds
Levelling compound is mixed with water or latex liquid, depending on the type being used.
The compound is mixed to the consistency required from mixing by the correct ratio.
The mix is poured on to the floor and smoothed over using a trowel.
To get a good finish, a spiked roller is rolled over the wet compound to release any air that is trapped, that had been created during the mixing process.

## Slide 32: Levelling/smoothing compounds
Levelling compound is mixed with water or latex liquid depending on the type being used.
Pouring the compound
Using a spiked roller

## Slide 33: Types of materials: sealant (silicon)
Sealants are designed to be used in areas where a waterproof seal is needed between two materials, where differential movement can occur.
Silicon sealant
Sealant being applied to a bath and tile intersection

## Slide 34: Uncoupling membrane
Tiling to timber-based backgrounds is not good practice and advised against according to British Standards.
When tiling to timber floor background, an uncoupling membrane should be installed over the existing floor surface.
An uncoupling membrane system provides an intermediate substrate between the tile covering and load-bearing substrate. It can be used over a variety of substrates, including timber, concrete, cementitious screeds and gypsum-based screeds. It is designed to neutralise lateral stresses that occur between the substrate and tile covering; it is not designed to accommodate differential vertical movement (deflection).
Notes: Source: https://www.schluter.co.uk

## Slide 35: Timber-based backgrounds
How does an uncoupling membrane work?
The membrane works by preventing stresses from the substrate being transferred into the tile covering that can cause cracking and delamination of the covering material.
As substrates will expand and contract due to changes in temperature and moisture levels, an uncoupling membrane is perfect for allowing the surfaces to move independently preventing stress on the tiles which can cause cracking or even debonding. This is because the membrane uncouples the floor covering from the substrate and neutralises the tensions between the substrate and the tile covering that result from the varying deformations of the materials. Likewise, stress cracks in the substrate are bridged and are, therefore, not transferred to the surface covering.
Notes: Source: https://www.schluter.co.uk

## Slide 36: Timber-based backgrounds: uncoupling membrane installation
Acrylic primer is applied to the timber substrate.
The uncoupling membrane is fixed to the timber substrate with flexible adhesive.
It is left to set.
Tiling is fixed to the membrane with flexible adhesive.

## Slide 37
Any questions?